## Slide 1: Introduction to In4SnS8 Nanosheets
- Overview of In4SnS8 nanosheets
- Applications in environmental remediation, solar energy conversion, and advanced nanodevices
- Importance in nanotechnology and material science

## Slide 2: Synthesis of In4SnS8 Nanosheets
- Synthesized via a thermal decomposition method
- Utilizes Sn(DDTC)4 and In(DDTC)3 in oleylamine solvent
- Heating process: 120°C under vacuum, followed by 240°C under N2 atmosphere

## Slide 3: Characterization Techniques
- Morphology examined using TEM (Tecnai G2 F30 S-Twin)
- XRD patterns for structural analysis (Bruker D8 Advance)
- XPS for elemental composition (PHI 5000 Versaprobe)

## Slide 4: Properties of In4SnS8 Nanosheets
- Ultrathin nature with an average thickness of 3.8 nm
- Comprises five atomically thick layers
- Large specific surface area of 40.34 m²/g

## Slide 5: Photocatalytic Efficiency
- Fast adsorption-visible-light photocatalysis dual function
- Effective for various organic dyes removal
- Potential for solar energy conversion and environmental remediation

## Slide 6: Comparative Analysis
- Higher efficiency compared to other structures like In4SnS8 microspheres
- Specific surface area significantly larger than flower-like microspheres (24.7 m²/g)

## Slide 7: Conclusion and Future Directions
- Promising advances in 2D nanomaterials
- Potential applications in environmental and energy sectors
- Continued research to optimize synthesis and application methods